## Problem 3: F&H 5.8 — Sharp Reaction Front Analysis

### Additional Required Assumption

Beyond the stated assumption that σ ≫ κ (Kr → 0, so ohmic resistance lies entirely in the electrolyte phase, forcing the reaction front toward the electrode/separator interface), the scenario of a sharp moving front also requires:

The reaction must be transport/kinetically fast relative to the rate of solid-phase consumption — i.e., ν² ≫ 1 (ohmically limited regime), so that the reaction is confined to a thin zone and the transition between fully-reacted and unreacted solid is sharp rather than distributed.

Physically: once the electrolyte current penetrates only a distance ~λ into the electrode, material within λ of the front reacts completely before the front advances. This requires the electrode capacity per unit volume to be large enough (or the current small enough) that the solid reactant is fully consumed locally before the front moves appreciably — a quasi-static front velocity assumption.

## Problem 4: LiMn₂O₄ Electrode Utilization Length

### Given Parameters

| Parameter | Value |
| --- | --- |
| Particle radius, r | 8.5 μm = 8.5×10⁻⁶ m |
| Porosity, ε | 0.30 |
| Exchange current density, i₀ | 10 A/m² |
| αa = αc | 0.5 → (αa + αc) = 1.0 |
| Effective electrolyte conductivity, κeff | 3.0 Ω⁻¹m⁻¹ |
| Solid conductivity, σ | → ∞ (highly conductive) |

a=3(1-ε)r=3(0.70)8.5×10-6=2.47×105 m-1

Since σ → ∞, the term (1/κ + 1/σ) → 1/κeff. The characteristic utilization length is:

λ2=RT⋅κeffa⋅i0⋅(αa+αc)⋅F

At T = 298 K (RT/F = 0.02569 V):

λ2=0.02569)(3.02.47×105)(10)(1.0=0.077072.47×106=3.12×10-8 m2
λ=1.77×10-4 m=177 μm

With electrode thickness L = 70 μm:

ν=Lλ=70 μm177 μm≈0.40

Since ν ≈ 0.4 < 1, the electrode is electrochemically thin.

Since the electrode thickness is 70 μm and the utilization length is 177 μm, we’ve got Le≪λ. In plain terms, the electrode is thin enough that transport doesn’t “choke” the reaction anywhere.

That implies:

- The reaction current is pretty uniform across the full thickness

- The active material is basically fully utilized — no real “dead zone” building up near the current collector

- Electrolyte-phase ohmic losses are small compared to the kinetic resistance (i.e., transport isn’t the limiting factor here)

This setup is ideal for a high C-rate / power application because:

- A thin electrode keeps ionic path lengths short → lower ohmic drop at high current density

- Uniform reaction means you don’t get early local depletion near the separator (no “front-loading” of the reaction)

If the goal is low C-rate / high capacity, you could push the thickness up toward (or past) λ≈177 μmto pack in more active material per area. You’d be accepting some reaction non-uniformity, but at slow rates that tradeoff is usually fine because the ohmic penalties stay manageable.

1) Clear, direct answers

1) Fuller & Harb Problem 5.2

For the porous electrode made from particles of intrinsic density ρsand apparent density ρa:

ρa=ρs(1-ε)

so

ε=1-ρaρs

Using ρs=2100 kg m-3and ρa=1260 kg m-3,

ε=1-12602100=0.40

For spherical particles of diameter 5.0 μm, the radius is r=2.5×10-6 m, and the specific interfacial area is

a=3(1-ε)r

so

a=3(0.60)2.5×10-6=7.2×105 m-1

For a 1 mm electrode, the true internal area relative to superficial area is

aL=(7.2×105)(1.0×10-3)=720

So the internal interfacial area is 720 times the superficial area. These come directly from the porosity and spherical-particle relations developed in Chapter 5.

Chapter 5

Part (b): tortuosity

Use the effective conductivity relation

κeff=κiετ

So

τ=κiεκeff
τ=9.7)(0.403.0=1.29

So the estimated tortuosity is

τ≈1.3

using the conductivity relation from the porous-media section.

Chapter 5

2) Fuller & Harb Problem 5.10

The key parameter is

ν2=ai0(αa+αc)FL2RT1κ1σ

and it is most useful to interpret it as

ν=Lλ

where λis the characteristic utilization length:

λ=RTai0(αa+αc)F1κ1σ1/2

So ν2is the square of “electrode thickness / utilization length,” or equivalently the inverse-Wagner-number type measure discussed in the chapter. Large νmeans the electrode is thick relative to how deeply reaction can penetrate; small νmeans the reaction penetrates through essentially the whole electrode.

Chapter 5

For part (b), sketching the magnitude of di2/dx(the local reaction rate/current-transfer density):

- Kr=1, ν2≫1: symmetric U-shaped profile. High reaction near both front and back, minimum in the middle.

- Kr=1, ν2≪1: nearly flat/uniform profile across the electrode.

- Kr=0.01, ν2≫1: strongly front-loaded profile. Very high near the front, then drops rapidly moving into the electrode, with very little reaction near the back.

That matches the behavior shown in the chapter’s current-distribution figures: equal conductivities give symmetry, while κ≪σpushes reaction toward the electrolyte side.

Chapter 5

3) Fuller & Harb Problem 5.8

Besides assuming σ≫κ, the other big assumption is that the electrode acts like it has a sharp, moving reaction front. Practically, that means the reaction/utilization zone is really thin compared to the electrode thickness:

λ≪Le

So the material right at the front gets basically used up before you see meaningful reaction deeper in the electrode. Said another way: the local kinetics/utilization are fast enough compared to ionic transport that you can treat the electrode as two regions — reacted and unreacted — separated by a narrow interface.

Chapter 5

A useful extra nuance: this picture also quietly assumes particle-scale diffusion inside the active material is not the dominant bottleneck. Otherwise the front would smear out instead of staying sharp.

4) Custom lithium-battery electrode problem

For spherical particles,

a=3(1-ε)r

with r=8.5×10-6 mand ε=0.30:

a=3(0.70)8.5×10-6=2.47×105 m-1

highly conductive, take σ≫κ, so

λ=RT κeffai0(αa+αc)F1/2

Using

- κeff=3.0 Ω-1m-1

- i0=10 A m-2

- αa=αc=0.5⇒αa+αc=1

- T≈298 K

gives

λ≈1.77×10-4 m=177 μm

With electrode thickness L=70 μm,

ν=Lλ=70177≈0.40

So this electrode is not electrochemically thick. It is closer to electrochemically thin, though not in the extreme limit. That means reaction should penetrate a substantial fraction of the electrode instead of being confined to a narrow region near the front. This follows directly from the utilization-length framework in the chapter.

Chapter 5

Because L<λ, this thickness is better suited to higher C-rate service than to maximum low-rate capacity. A thicker electrode would pack in more active material for low-rate/high-capacity use, but it would also push the design toward nonuniform utilization and stronger transport losses.

Chapter 5

2) Step-by-step explanation of how I got there

Problem 5.2

Chapter 5 gives:

- porosity definition ε

- spherical-particle area relation a=3(1-ε)/r

- conductivity relation κeff=κiε/τ

Chapter 5

So the workflow is:

- Get porosity from density:

ε=1-ρa/ρs

- Use particle radius in the spherical-area formula to get a.

- Multiply aby thickness Lto convert “area per volume” into “total true area / superficial area.”

- Use the measured conductivity ratio to back out tortuosity.

That is the whole game. No mystery, just geometry plus effective transport.

Problem 5.10

The hint you were given is exactly the right move:

ν=Lλ

So instead of treating ν2as some ugly algebraic blob, read it as:

- small ν→ utilization length is large compared with the electrode thickness → reaction reaches throughout the electrode

- large ν→ utilization length is small compared with the electrode thickness → reaction localizes where resistance is smallest

Then Kr=κ/σtells you which side is favored:

- Kr=1: neither phase is favored → symmetric profile

- Kr<1: electrolyte is less conductive than solid → reaction favors the front

- Kr>1: solid is less conductive than electrolyte → reaction favors the back

Chapter 5

Problem 5.8

The sharp-front picture is stronger than just saying “electronic conduction is easy.”
You also need the reaction zone to be narrow, meaning the electrode is thick relative to the penetration depth. Otherwise the reaction would still be distributed over a finite region instead of looking like that clean reacted/unreacted split.

So the hidden assumption is basically:

sharp-front approximation  ⟺  λ≪Le

That is the real structural assumption behind the figure.

Custom lithium electrode

Same logic as 5.10, but now you were given actual numbers.

- Compute afrom particle size and porosity.

- Use the utilization-length expression.

- Since particles are highly conductive, simplify with σ≫κ.

- Compare λto L.

You got:

- a≈2.47×105 m-1

- λ≈177 μm

- L=70 μm

- ν≈0.40

Since the thickness is well below the utilization length, the electrode is more rate-capable than a thick, capacity-maximized design.

3) Alternative perspectives or solutions

For 5.2(b)

A nice check is the Bruggeman estimate:

κeffκi≈ε1.5

For ε=0.40,

ε1.5≈0.253

so Bruggeman would predict

κeff≈9.7(0.253)≈2.45 S m-1

Measured was 3.0 S m-1, so your pore network appears a bit less tortuous / more transport-friendly than the simple Bruggeman approximation would suggest. That is a good sanity check from the same chapter.

Chapter 5

For the lithium electrode

If you did not assume σ≫κ, then you would use

λ=RTai0(αa+αc)F1κ1σ1/2

That would make λa bit smaller if the solid-phase conductivity were not huge. So my estimate is slightly optimistic on rate capability—but that is exactly the assumption the problem wording invites.

4) Practical summary / action plan

Here are the final boxed results to submit:

ε=0.40
a=7.2×105 m-1for Problem 5.2
Area increase factor=aL=720
τ≈1.29
ν=Lλ,λ=RTai0(αa+αc)F1κ1σ1/2
5.10 meaning of ν2: thickness-to-utilization-length ratio squared
5.8 extra assumption: sharp-front behavior (λ≪Le)
a=2.47×105 m-1for the Li electrode
λ≈177 μm
ν≈0.40⇒closer to electrochemically thin than thick
70 μm is better for higher C-rate than for maximum low-rate capacity

If you want, I can turn this into a clean homework-style submission with polished prose, equations, and simple sketches for the 5.10 profiles.

Sources